SUPPORTING INFORMATION

DFT study of Host-Dopant systems of DPVBi with Organophosphorus π-Conjugated materials

Anusha Valabojua, Krishna Chaitanya Gunturub, Bhanuprakash Kotamarthia*

aInorganic and Physical Chemistry Division and Acsir, CSIR-Indian Institute of Chemical Technology, Hyderabad 500 007, India. *E-mail: bprakash@iict.res.in

bSchool of Chemical Sciences, Swami Ramanand Teerth Marathawada University, Nanded, Maharashtra, India.

and

# Damien Jolyc, Muriel Hisslerc*

cInstitut des Sciences Chimiques de Rennes, UMR 6226, CNRS-Université de Rennes 1, Campus de Beaulieu, 35042 Rennes Cedex, France. muriel.hissler@univ-rennes1.fr

Contents

Table S1. Selected bond lengths (A°), torsional angles (Ф, (°)) and dipole moments (Debye) of ground state (GS) and excited state (ES) geometries of DPVBi, Phospholes A and B at B3LYP/6-31+G(d,p) level in dichloromethane solvent in comparison with X-ray data.......................................................................................................................................(2)

Figure S1. Frontier molecular Orbitals (Energies in eV) of homodimers DPVBi, A and B calculated at B3LYP/6-31+g(d,p) level of theory in gas phase (isovalue=0.02)................................................................................................(3)

Figure S2. Frontier molecular Orbitals (Energies in eV) of heterodimers DPVBi-A(DA) and DPVBi-B(DB) calculated at B3LYP/6-31+G(d,p)//B97D/6-31G(d) level of theory (isovalue=0.02).......................................................................(5)

Figure S3. Scheme to calculate reorganization energy(eV).........................................................................................(9)

Table S2. Selected bond lengths (A°) and torsional angles (°) of DPVBi, Phospholes A and B at B3LYP/6-31+g(d,p) level in gas phase along with respective cation and anion optimized geometries......................................................(10)

Table S3. The calculated Interaction energies (∆Eintcp, in kcal/mol), Effective charge transfer integrals ((Jeff)ij in eV), for hole and electron transfer of heterodimers DPVBi-A (DA) and DPVBi-B(DB)............................................................(12)

Figure S4. Frontier molecular Orbitals (Energies in eV) of DPVBi, Phospholes A and B calculated at B3LYP/6-31+G(d,p) level of theory in dichloromethane solvent (isovalue=0.02).......................................................................(16)

Figure S5. Natural Transition Orbitals (Energies in eV) of DPVBi, Phospholes A and B calculated at CAM-B3LYP and M06-2X functionals  and 6-31+G(d,p) level of theory in dichloromethane solvent (isovalue=0.02).....................(17)

Table S1. Selected bond lengths (A°), torsional angles (Ф, (°)) and dipole moments (Debye) of ground state (GS) and excited state (ES) geometries of DPVBi, Phospholes A and B at B3LYP/6-31+G(d,p) level in dichloromethane solvent in comparison with X-ray data.

| DPVBi Phospholes A and B |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Bond | DPVBi |  |  | Bond | A |  |  | B |  |  |
|  | GS | ES | Expa. |  | GS | ES | Expb. | GS | ES | Expb. |
| 1 | 1.483 | 1.438 | 1.481 | P-S | 1.993 | 2.025 | 1.953 | 1.995 | 2.028 | 1.953 |
| 2, 2’ | 1.407, 1.409 | 1.436, 1.435 | 1.387, 1.393 | P-C1 | 1.838 | 1.843 | 1.818 | 1.836 | 1.842 | 1.816 |
| 3, 3’ | 1.409, 1.408 | 1.435, 1.436 | 1.393, 1.387 | P-C2 | 1.839 | 1.815 | 1.814 | 1.843 | 1.814 | 1.820 |
| 4, 4’ | 1.392, 1.392 | 1.374, 1.375 | 1.373, 1.368 | P-C5 | 1.828 | 1.810 | 1.799 | 1.823 | 1.810 | 1.800 |
| 5, 5’ | 1.392, 1.392 | 1.375, 1.374 | 1.368, 1.373 | C3-C2 | 1.369 | 1.438 | 1.358 | 1.37 | 1.436 | 1.361 |
| 6, 6’ | 1.410, 1.410 | 1.433, 1.433 | 1.393, 1.383 | C3-C4 | 1.489 | 1.409 | 1.479 | 1.491 | 1.409 | 1.491 |
| 7, 7’ | 1.410, 1.410 | 1.433, 1.433 | 1.383, 1.393 | C4-C5 | 1.362 | 1.440 | 1.355 | 1.359 | 1.440 | 1.350 |
| 8, 8’ | 1.470, 1.471 | 1.426, 1.426 | 1.465, 1.465 | C2-C7 | 1.448 | 1.418 | 1.45 | 1.446 | 1.416 | 1.452 |
| 9, 9’ | 1.360, 1.360 | 1.400, 1.400 | 1.352, 1.352 | C5-C6 | 1.476 | 1.432 | 1.479 | 1.480 | 1.435 | 1.481 |
| 10, 10’ | 1.491, 1.491 | 1.470, 1.470 | 1.482, 1.482 |  |  |  |  |  |  |  |
| 11, 11’ | 1.495, 1.495 | 1.478, 1.478 | 1.484, 1.484 |  |  |  |  |  |  |  |
| Ф1 | -33.6 | -3.0 | 0.8 | Ф1 | 17.1 | -5.4 | 17.7 | -5.4 | -11.2 | 1.2 |
| Ф2 | 8.6 | 19.5 | 3.3 | Ф2 | 53.6 | 20.4 | 52.4 | 64.1 | 27.9 | 62 |
| Ф3 | -8.4 | -19.6 | -3.3 |  |  |  |  |  |  |  |
| Dipole moment | 0.21 | 0.04 |  |  | 6.45 | 6.22 |  | 8.02 | 7.87 |  |
| aSee ref no.66, bSee ref no. 11 |  |  |  |  |  |  |  |  |  |  |

Figure S1. Frontier molecular Orbitals (Energies in eV) of homodimers DPVBi, A and B calculated at B3LYP/6-31+g(d,p) level of theory in gas phase (isovalue=0.02).

|  | HOMO-1 | HOMO | LUMO | LUMO+1 |
| --- | --- | --- | --- | --- |
| DD1 | -5.4 | -5.37 | -1.87 | -1.84 |
| DD2 | -5.36 | -5.36 | -1.84 | -1.82 |
| DD3 | -5.38 | -5.37 | -1.85 | -1.83 |
| DD4 | -5.39 | -5.38 | -1.86 | -1.85 |
| AA1 | -5.48 | -5.21 | -2.25 | -2.02 |
| AA2 | -5.47 | -5.32 | -2.22 | -2.11 |
| AA3 | -5.55 | -5.29 | -2.33 | -2.06 |
| AA4 | -5.59 | -5.23 | -2.38 | -1.97 |
| AA5 | -5.41 | -5.34 | -2.16 | -2.14 |
| BB1 | -5.49 | -5.44 | -2.2 | -2.07 |
| BB2 | -5.32 | -5.26 | -2.01 | -1.96 |
| BB3 | -5.31 | -5.11 | -1.97 | -1.94 |
| BB4 | -5.26 | -5.18 | -1.97 | -1.95 |

Figure S2. Frontier molecular Orbitals (Energies in eV) of heterodimers DPVBi-A(DA) and DPVBi-B(DB) calculated at B3LYP/6-31+G(d,p)//B97D/6-31G(d) level of theory (isovalue=0.02).

|  | HOMO-1 | HOMO | LUMO | LUMO+1 |
| --- | --- | --- | --- | --- |
| DA1 | -5.35 | -5.33 | -2.37 | -2.02 |
| DA2 | -5.41 | -5.25 | -2.43 | -1.96 |
| DA3 | -5.35 | -5.31 | -2.39 | -1.96 |
| DA4 | -5.25 | -5.16 | -2.45 | -1.97 |
| DA5 | -5.36 | -5.32 | -2.46 | -2.01 |
| DA6 | -5.43 | -5.4 | -2.32 | -2.11 |
| DA7 | -5.42 | -5.34 | -2.35 | -2.11 |
| DA8 | -5.43 | -5.26 | -2.48 | -2.04 |
| DA9 | -5.33 | -5.19 | -2.43 | -2.1 |
| DA10 | -5.37 | -5.29 | -2.41 | -1.98 |
| DA11 | -5.41 | -5.36 | -2.44 | -2.06 |
| DA12 | -5.36 | -5.3 | -2.47 | -2.02 |
| DA13 | -5.39 | -5.28 | -2.5 | -1.99 |
| DA14 | -5.36 | -5.3 | -2.47 | -2.02 |
| DA15 | -5.32 | -5.23 | -2.46 | -1.96 |
| DA16 | -5.44 | -5.4 | -2.34 | -2.08 |
| DA17 | -5.48 | -5.24 | -2.37 | -2.24 |
| DA18 | -5.41 | -5.35 | -2.38 | -2.02 |
| DA19 | -5.44 | -5.32 | -2.46 | -2.05 |
| DA20 | -5.42 | -5.32 | -2.31 | -1.96 |
| DB1 | -5.29 | -5.23 | -2.41 | -1.93 |
| DB2 | -5.29 | -5.21 | -2.28 | -1.93 |
| DB3 | -5.53 | -5.37 | -2.25 | -2.17 |
| DB4 | -5.35 | -5.22 | -2.29 | -2.0 |
| DB5 | -5.38 | -5.36 | -2.31 | -2.08 |
| DB6 | -5.4 | -5.34 | -2.3 | -2.03 |
| DB7 | -5.39 | -5.19 | -2.24 | -2.0 |
| DB8 | -5.53 | -5.21 | -2.23 | -2.21 |
| DB9 | -5.41 | -5.19 | -2.38 | -1.85 |
| DB10 | -5.39 | -5.14 | -2.32 | -1.9 |
| DB11 | -5.34 | -5.26 | -2.28 | -1.97 |
| DB12 | -5.42 | -5.22 | -2.41 | -2.02 |

Figure S3. Scheme to calculate reorganization energy (eV).

| DPVBi |  |  |  |  |
| --- | --- | --- | --- | --- |
| Bond | DPVBi |  |  |  |
|  | GS | Optimized cation | Optimized anion | Exp.a |
| 1 | 1.482 | 1.457 | 1.456 | 1.481 |
| 2, 2’ | 1.407, 1.408 | 1.420, 1.422 | 1.424, 1.424 | 1.387, 1.393 |
| 3, 3’ | 1.408, 1.407 | 1.421, 1.420 | 1.424, 1.423 | 1.393, 1.387 |
| 4, 4’ | 1.392, 1.391 | 1.380, 1.379 | 1.382, 1.383 | 1.373, 1.368 |
| 5, 5’ | 1.391, 1.392 | 1.379, 1.379 | 1.382, 1.383 | 1.368, 1.373 |
| 6, 6’ | 1.410, 1.410 | 1.423, 1.423 | 1.425, 1.424 | 1.393, 1.383 |
| 7, 7’ | 1.410, 1.410 | 1.423, 1.423 | 1.425, 1.424 | 1.383, 1.393 |
| 8, 8’ | 1.470, 1.470 | 1.442, 1.442 | 1.442, 1.441 | 1.465, 1.465 |
| 9, 9’ | 1.359, 1.359 | 1.383, 1.383 | 1.386, 1.387 | 1.352, 1.352 |
| 10, 10’ | 1.490, 1.490 | 1.475, 1.475 | 1.476, 1.476 | 1.482, 1.482 |
| 11, 11’ | 1.494, 1.494 | 1.483, 1.484 | 1.487, 1.487 | 1.484, 1.484 |
| Ф1 | 143.9 | -158.2 | -161.7 | 180.0 |
| Ф2 | -174.0 | -168.6 | -168.7 | -179.4 |
| Ф3 | 173.8 | 168.5 | 168.6 | 179.4 |
| a See ref no. 66 |  |  |  |  |

Table S2.a. Selected bond lengths (A°) and torsional angles (°) of DPVBi at B3LYP/6-31+g(d,p) level in gas phase along with respective cation and anion optimized geometries. (Values in parentheses are experimental measures from X-ray diffraction studies)

Table S2.b. Selected bond lengths (Å) and torsional angles (°) of Phospholes A and B at B3LYP/6-31+g(d,p) level in gas phase along with respective cation and anion optimized geometries. (Values in parentheses are experimental measures from X-ray diffraction studies)

| Phospholes A and B |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Bond | A |  |  |  | B |  |  |  |
|  | GS | Optimized cation | Optimized anion | Expa. | GS | Optimized cation | Optimized anion | Expa. |
| P=S | 1.978 | 1.969 | 2.015 | 1.953 | 1.980 | 1.969 | 2.018 | 1.953 |
| P-C1 | 1.842 | 1.829 | 1.858 | 1.818 | 1.840 | 1.828 | 1.856 | 1.816 |
| P-C2 | 1.844 | 1.850 | 1.819 | 1.814 | 1.846 | 1.852 | 1.818 | 1.820 |
| P-C5 | 1.830 | 1.848 | 1.811 | 1.799 | 1.829 | 1.85 | 1.811 | 1.800 |
| C3-C2 | 1.369 | 1.403 | 1.414 | 1.358 | 1.368 | 1.402 | 1.411 | 1.361 |
| C3-C4 | 1.488 | 1.443 | 1.429 | 1.479 | 1.490 | 1.446 | 1.431 | 1.491 |
| C4-C5 | 1.362 | 1.403 | 1.415 | 1.355 | 1.359 | 1.398 | 1.413 | 1.350 |
| C2-C7 | 1.446 | 1.417 | 1.432 | 1.450 | 1.447 | 1.413 | 1.433 | 1.452 |
| C5-C6 | 1.475 | 1.437 | 1.449 | 1.479 | 1.478 | 1.443 | 1.453 | 1.481 |
| Ф1 | -166.0 | -176.5 | -180.0 | -162.6 | 163.4 | 172.4 | 159.8 | -177.1 |
| Ф2 | -132.0 | -155.9 | -155.3 | -130.9 | -116.4 | -145.3 | -145.6 | -121.4 |
| a ref no. 11 |  |  |  |  |  |  |  |  |

Table S3. The calculated Interaction energies (∆Eintcp, in kcal/mol), Effective charge transfer integrals ((Jeff)ij in eV) for hole and electron transfer of heterodimers DPVBi-A(DA) and DPVBi-B(DB).a,b

| DA |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| DA1 CH- π: 3.594, 2.426, 2.509, 3.743, 3.067, 3.014, 3.842, 2.874 Å ∆Eint = -28.90, δEABBSSE= 11.59, ∆EintCP = -17.31 J+ = 4.11 x10-3, J- = -4.89 x10-3 | DA2 π-π: 3.725 Å CH- π: 3.455, 3.262, 2.747 Å ∆Eint = -21.58, δEABBSSE= 9.73, ∆EintCP = -11.85 J+ = 7.14 x10-3, J- = 7.48 x10-3 |  | DA3 CH- π: 3.870, 3.853, 2.946, 3.733, 3.138, 3.515, 3.869, 2.744 ∆Eint = -19.68, δEABBSSE= 7.82, ∆EintCP =-11.86 J+ = -1.01 x10-2, J- = 1.96 x10-2 |  |  |
| DA4 π -π: 3.662 Å CH- π: 3.641, 3.376, 3.703 Å CH-PS : 3.800 Å, ∆Eint = -24.39, δEABBSSE= 9.64, ∆EintCP = -14.75 J+ = 4.16 x10-2, J- = -1.43 x10-3 | DA5 CH-π: 3.356, 3.457, 3.745 Å CH-PS: 2.972 Å, ∆Eint = -8.84, δEABBSSE= 3.34, ∆EintCP = -5.49 J+ = -1.20 x 10-4 , J- = 2.23 x10-3 |  | DA6 CH-π: 2.962, 3.293, 3.489, 3.455, 3.057, 3.541 Å ∆Eint =-23.81, δEABBSSE= 8.62, ∆EintCP = -15.19 J+ = 3.80 x10-4, J- = -7.28 x10-3 |  |  |
| DA7 π-π 3.947 Å, CH-π: 3.787, 3.383, 3.840, 3.031, 3.583, 3.963, 2.798, 3.353, 3.011 Å ∆Eint = -23.48, δEABBSSE= 9.89, ∆EintCP = -13.59 J+ = -2.93 x10-2, J- = -5.17 x10-3 | DA8 CH-π: 3.166, 3.694, 3.223, 3.079, 3.375, 3.528, 2.799, 2.556, 3.353, 3.792 Å ∆Eint = -28.93, δEABBSSE=11.86, ∆EintCP = -17.07 J+ = -7.08 x10-2, J- = -2.24 x10-2 |  | DA9 CH-π: 2.496, 3.766, 3.660, 3.680, 3.558, 3.845, 3.994, 2.517, 3.305, 3.355, 3.481 Å ∆Eint = -23.32,δEABBSSE= 9.48, ∆EintCP = -13.85 J+ = -1.17 x10-2, J- = 5.99 x10-3 |  |  |
| DA10 CH-π: 3.935, 3.782, 3.421, 3.579, 3.915, 3.649, 2.381, 2.844, 2.611, 3.127 Å ∆Eint =-27.62, δEABBSSE=11.14, ∆EintCP =-16.48 J+ = -2.89 x10-2, J- = 7.93 x10-3 | DA11 CH –π: 3.585, 3.383, 3.675, 3.006, 2.541, 2.919 ∆Eint = -13.78,δEABBSSE= 5.83, ∆EintCP = -7.94 J+ = -1.22 x10-2, J- = -5.19 x10-3 |  | DA12 CH –π: 2.766, 3.806, 3.289, 3.207 π –π 3.617 Å, ∆Eint = -17.79, δEABBSSE=7.52, ∆EintCP=-10.27 J+ = 1.04 x10-2, J- = 1.02 x10-2 |  |  |
| DA13 CH –π: 2.544, 3.741, 3.229, 3.288 π –π 3.585 Å, ∆Eint = -27.86, δEABBSSE=11.58, ∆EintCP =-16.28 J+ =1.29 x10-3, J- = 2.72 x10-2 | DA14 CH –π: 2.766, 3.735, 3.289, 3.207 Å π –π 3.616 Å, ∆Eint = -17.79, δEABBSSE= 7.52, ∆EintCP = -10.27 J+ = 1.04 x10-2, J- = 1.02 x10-2 |  | DA15 CH –π: 3.654, 3.664, 3.833, 3.427 π –π 3.778 Å, ∆Eint = -18.50,δEABBSSE=7.32, ∆EintCP =-11.18 J+ = -1.31 x10-2, J- = -1.05 x10-2 |  |  |
| DA16 CH –π: 3.673, 3.466, 3.147, 3.285, 3.639, 3.176, 3.786, 3.443, 3.978 Å CH-P-ring: 2.977 Å ∆Eint = -23.67, δEABBSSE= 8.84, ∆EintCP =-14.83 J+ = 5.80 x10-4, J- = -1.30 x10-2 | DA17 CH –π: 3.336, 3.163, 3.378, 3.488, 2.721, 3.279, 3.661 Å CH-P-ring: 3.155 Å π –π 3.689 Å ∆Eint = -27.19, δEABBSSE= 11.65, ∆EintCP =-15.54 J+ = 5.68 x10-2, J- = -1.71 x10-3 |  | DA18 CH –π: 2.802, 2.542, 3.392, 3.718 Å. ∆Eint = -14.00, ,δEABBSSE= 5.02,∆EintCP =-8.97 J+ = 2.09 x10-2, J- = -2.21 x10-2 |  |  |
| DA19 π-π 3.599 Å, CH- π: 3.981, 2.884, 2.517, 2.419, 3.336, 3.203, 2.979 Å ∆Eint =-30.09,δEABBSSE= 11.49, ∆EintCP =-18.60 J+ = -1.26 x10-2, J- = -4.30 x10-3 | DA20 CH- π : 3.832, 3.580, 3.513, 3.132, 2.611, 3.593, 3.876, 3.057, 2.780 Å ∆Eint = -26.70,δEABBSSE=10.63, ∆EintCP = -16.07 J+ = 3.72 x10-3, J- = -5.55 x10-3 |  |  |  |  |
| DB |  |  |  |  |
| DB1 CH-π: 2.707, 2.544, 3.229 Å ∆Eint = -13.63,δEABBSSE= 4.78, ∆EintCP = -8.85 J+ = -1.39 x10-2, J- = -8.35 x10-3 |  | DB2 π-π 3.829 Å CH-π: 3.015, 2.442, 2.532, 3.829, 3.153, 2.502, 2.834 Å ∆Eint = -26.84, δEABBSSE=11.71, ∆EintCP = -15.13 J+ = -1.84 x10-2, J- = 2.94 x10-2 |  | DB3 CH-π: 3.342, 3.914, 3.906, 3.472, 3.172, 3.346, 3.342 Å. ∆Eint = -26.61,δEABBSSE=11.02, ∆EintCP = -15.59 J+ = -2.40 x10-2, J- = -7.03 x10-3 |
| DB4 π-π 3.807 Å, CH-π: 3.362, 2.978, 3.501, 3.362 Å ∆Eint = -20.55, δEABBSSE=7.69, ∆EintCP = -12.86 J+ = 5.30 x10-2, J- = -1.60 x10-2 |  | DB5 CH-PS 2.882 Å, CH-π : 3.071, 2.683 Å ∆Eint = - 15.08, δEABBSSE= 5.24, ∆EintCP = -9.84 J+ = 8.52 x10-3, J- = 1.29 x10-2 |  | DB6 CH-π 2.797 Å, CH-π : 3.660, 2.778, 3.171, 2.879, 2.933, 2.335, 2.890 Å ∆Eint = - 24.71,δEABBSSE= 8.77, ∆EintCP = -15.94 J+ = -4.85 x10-3, J- = 2.60 x10-2 |
| DB7 π-π 3.497 Å, CH-π : 3.468, 3.056, 3.826, 3.587, 3.295, 2.948, 3.061, 3.986, 3.198 Å ∆Eint = -28.57,δEABBSSE= 12.26, ∆EintCP= -16.30 J+ = -2.97 x10-2, J- = 3.44 x10-2 |  | DB8 CH- π: 3.401, 3.667, 3.650, 3.754, 3.774 Å ∆Eint = -14.30, δEABBSSE= 5.19, ∆EintCP = -9.11 J+ = -1.23 x10-03, J- = -5.01 x10-3 |  | DB9 π-π 3.863, CH- π : 3.476, 3.509, 3.898, 2.413, 3.181 Å ∆Eint =-25.57,δEABBSSE=10.76, ∆EintCP = -14.81 J+ = -2.53 x10-2, J- = 3.33 x10-2 |
| DB10 π-π 3.857 Å, CH- π : 3.568, 2.467, 3.209 Å ∆Eint = -17.89, δEABBSSE= 7.04, ∆EintCP = -10.84 J+ = 4.40 x10-4, J- = 4.55 x10-3 |  | DB11 CH- π : 2.931, 2.557, 3.719 Å ∆Eint = -18.80,δEABBSSE= 7.06, ∆EintCP = -11.74 J+ = -1.61 x10-2, J- = -2.43 x10-2 |  | DB12 π - π: 3.603 CH- π : 2.510, 2.885, 3.531, 3.204,2.976 Å ∆Eint = -30.14, δEABBSSE= 11.49 ∆EintCP =-18.65 J+= 1.24 x10-2, J-= -4.53 x10-3 |
| a ∆Eintcp in kcal/mol obtained at B2PLYPD/6-31G(d,p)//B97D/6-31g(d) level. b Rest of quantities obtained at B3LYP/TZ2P level of theory |  |  |  |  |

Figure S4. Frontier molecular Orbitals (Energies in eV) of DPVBi, Phospholes A and B calculated at B3LYP/6-31+G(d,p) level of theory in dichloromethane solvent (isovalue=0.02).

|  | DPVBi | A | B |
| --- | --- | --- | --- |
| LUMO+2 | -0.8 | -1.19 | -1.17 |
| LUMO+1 | -1.48 | -1.3 | -1.31 |
| LUMO | -2.02 | -2.42 | -2.33 |
| HOMO | -5.58 | -5.62 | -5.56 |
| HOMO-1 | -6.07 | -6.22 | -6.14 |
| HOMO-2 | -6.95 | -6.48 | -6.42 |

Figure S5.a. Natural Transition Orbitals (Energies in eV) of DPVBi, Phospholes A and B calculated at CAM-B3LYP/6-31+G(d,p) level of theory and dichloromethane solvent (isovalue=0.02) .

| CAM-B3LYP | DPVBi | A | B |
| --- | --- | --- | --- |
| LUMO |  |  |  |
| HOMO |  |  |  |

Figure S5.b. Natural Transition Orbitals (Energies in eV) of DPVBi, Phospholes A and B calculated at M06-2X/6-31+G(d,p) level of theory and dichloromethane solvent (isovalue=0.02).

| M06-2X | DPVBi | A | B |
| --- | --- | --- | --- |
| LUMO |  |  |  |
| HOMO |  |  |  |